一、選擇題 (每題3分，共30分)

1.對於金屬的敘述，何者有誤？

(A)金屬有延展性  (B)金屬易於加工成型  (C)金屬具有脆性

(D)金屬表面具光澤，並有良好導電性

2.下列哪種缺陷不屬於點晶體缺陷？

(A)插入型原子    (B)置入型原子    (C)空位    (D)差排

3.下列何者為退火處理的過程？

(A)回復      (B)再結晶       (C)晶粒成長       (D)以上皆是

4.下列何種金屬對X光線與原子輻射線有特殊遮斷力？

(A)鐵        (B)鋁           (C)鉛          (D)銅

5.黃銅是銅與下列何種金屬所構成的合金？

(A)鋅        (B)鋁           (C)錫          (D)鎳

6.下列何種金屬，導電性最佳？

(A)金        (B)銀           (C)銅          (D)鐵

7.凝固的熱力學條件為？

(A)能量守恆  (B)成核率       (C)系統自由能增加   (D)過冷度

8.費克第一定律描述了穩態擴散的特徵，即系統濃度不隨何者而改變？

(A)距離      (B)時間         (C)溫度        (D)以上皆是

9.一般安全玻璃的製作，通常在熱處理過程中進行哪一道程序？

(A)退火      (B)淬火         (C)回火        (D)過火

10.下列何者不是析出強化過程的步驟之一？

(A)固溶化    (B)回復         (C)淬火        (D)時效

二、簡答題

1.名詞解釋(10分)

(a)熱固性塑膠   (b)熱塑性塑膠   (c)平衡相圖

(d)法蘭克缺陷   (e)潛變

2.一般的液體金屬，固體顆粒成核機制有哪兩種? 請敘述。(10分)

3. (a) Is it possible to grind up and reuse phenol-formaldehyde? Why or why not? (10分)

.(b) Is it possible to grind up and reuse polypropylene? Why or why not? (10分)

4. Determine the ASTM grain size number if 30 grains per square inch are measured at a magnification of 250. (10分)

5. Briefly explain how each of the following influences the tensile modulus of a semicrystalline polymer and why: (20分)

(a) Molecular weight

(b) Degree of crystallinity

(c) Deformation by drawing

(d) Annealing of an undeformed material

(e) Annealing of a drawn material

# Text boxes

綠色能源科技學系碩士班

國立臺南大學105學年度     　    　　　　　　　　 招生考試  材料科學  試題卷